SPECIFICATIONS

V-10 SYSTEM

PART I -- GENERAL 1.00 SCOPE: This is a Manufacturer’s Specification on the Playground version of the VITRITURF V-10 System. 1.01 DESCRIPTION: Provide all labor, materials and equipment necessary to install the VITRITURF System. 1.02 QUALITY ASSURANCEA. Qualifications1. VITRITURF shall have marketed this system in the United States for at least five years.2. The Manufacturere shall be the Applicator and provide a single source warranty for materials and labor. B. Design and Detailing1. Generala. VITRITURF V-10 Playground System is utilized wherever an impact, absorbing cushioned surface is required. Playground areas should meet criteria set by the CPSC.2. Substrate and Substrate Systemsa. Check application manual for specific instructions on substrate.3. Acceptable Substrates for the VITRITURF V-10 System include asphalt. concrete and compacted stone.4. Other Substrates shall be approved by VITRITURF prior to application.5. The Trained Applicator shall verify that the proposed Substrate is acceptable with application of the VITRITURF System.6. Substrate Systems shall be engineered with regard to structural performance.7. Follow VITRITURF's published details with specific recommendations for this project. 1.03 SUBMITTALS:A. Trained Applicator shall submit 6” x 6” 1220mm) samples of the VITRITURF System. 1.04 DELIVERY, STORAGE AND HANDLINGA. Deliver all materials in original unopened packages with labels intact. B. Store all materialsprotected from weather and at temperature not less than 40 F (4 C). 1.05 JOB CONDITIONS:A. Ambient air temperature should be 32 F at the time of installation of the VITRITURF System.The System may be installedwith temperatures below 40. The temperature only affects the system in workability of the materials and the dry time. The lower the temperature, the thicker the viscosity of the binder and the dry time may become delayed.B. Tthe VITRITURF System shall be protected during installation while curing and/or unattended from weather and other damage. 1.06 ALTERNATES AND ALLOWANCES:A. Systems to be considered equal to those specified herein shall be approved by then Architect, in writing, at least ten working days prior to the project bid date. PART II -- PRODUCTS 2.01 GENERAL: All components of the VITRITURF V-10 System shall be obtained from VITRITURF or its authorized distributors. No substitutions of, or additions of, other materials shall be submitted without prior written permission from VITRITURF. 2.02 MATERIALSA. VITRITURF Primer: A single component moisture cured polyurethane primer.B. VITRITURF BINDER: A proprietary, elastic Polyurethane Pre-Polymer, MDI based. Extremely low odor, capable of excellentweathering and binding characteristics. Binder shall contain no TDI Monomers.C. VITRITURF Black SBR or Base Mat: Shall be recycled SBR Rubber, shall be cryogenically processed, be chopped to 1-3mm or 3/8"shredded granules and contain less than 4% dust and shall be packed in suitable bags to protect SBR from moisture.Base Mat- A combination of post consumer, non-tire shredded rubber with various sizings. The Base Mat shall be granular in appearance and provide for a flat base for the Vitriturf V-10 Wearing Course.D. VITRITURF V-10 EPDM Rubber: A man-made rubber containing minimum of 30% EPDM and having a density of 1.5-0.05.1. Is available in assorted colors and available in three sizes: 1-3mm, 0.5-1.5mm and 0.40-08mm (dust). A predetermined combination of sizes from Hanover Specialities Inc. will ensure proper wearing course to meet the requirements for issuance ofa TEN Year Warranty. E. The VITRITURF Playground System shall have been tested for shock attenuation under ASTM-F-1292 and HIC. Tested for non slip characteristics under ASTM-E303, ease of ignition under BS-5696 and ASTM-D-2859 for fire resistance under UL94. 2.03 MIXING AND PREPARATION: A. Mixture of binder/EPDM or binder/SBR will be determined by the system which is specified. PART III-- EXECUTION 3.01 INSPECTION:A. Prior to application of VITRITURF System the Substrates shall be examined for compliance with the contract documentsof VITRITURF specifications. The General Contractor and Architect shall be advised of all discrepancies. Work shall not proceed until unsatisfactory conditions are corrected. 3.02 INSTALLATION:VITRITURF Playground System1. VITRITURF Primer Apply primer with a short nap roller at a rate of 300 sq. ft. per gallon. 2. VITRITURF SBR Base Mata. Mix SBR to VITRITURF Binder in a ratio of 82/18 and spread evenly at specified thickness. Compact and allow to dry for 24 hours. 3. VITRITURF PrimerApply VITRITURF Primer at the rate of 300 so. ft. per gallon. 4. VITRITURF V-10 Wearing Coursea. Mix EPDM to VITRITURF Binder in a ratio of 82/18b. Apply with a steel trowel1. For compacting: Lubricate trowel with diesel fuel or soapy water.2. For finishing: Spray a light mist of water on surface and trowel smooth. Apply at a minimum of 1".